## Slide 1: DoE Cleanser Screening Tests First Cleanser using Triethanolamine Preliminary
W. Collins
C2E2
2014 September 23

## Slide 2: Objective
The objective of this screening test is to conduct a compatibility test between this compound and PEM fuel cells.
The testing is done in support of a supplement to a US DoE EERE contact, DE-EE0000467.
The results indicate some interaction between the compound and PEM fuel cells at the concentration and flow tested.

## Slide 3: Test parameters
Cell
Size 25 cm2
Electrode Gore-50
Loadings 0.4/0.4 mgPt/cm2
Operation
Current Density 1000 mA/cm2
Cell Temperature 800C
Inlet dew points
Anode 480C
Cathode 870C
Exit Pressures Ambient/Ambient

## Slide 4: Test parameters (cont)
Conditions
Flows
Anode 1.75 lpm (10)
Cathode 1.55 lpm (4)
Atomizer 130e-06 lpm
(~200 ppm)
Operating Point
Intentionally close to flooding
(worst case)
Program
Break in 16 hr hold @600 mV Diagnostics 5 hrs
Baseline 45 hr hold @1000 mA/cm2 Diagnostics 1 hr
Contamination 6 hrs
Diagnostics 1 hr
Clean up 24 hrs
Diagnostics 5 hr
Total 103 hrs

## Slide 5: Compound
Concentration 5% of full strength
  (estimate after two rinses)
Composition MSDS
Ingredient | CAS Number | Percent Range
Water | 7732-18-5 | ≥ 78%
Triethanolamine | 102-71-6 | ≤ 10%
Ethoxylated Alcohol | 68439-46-3 | ≤ 5%
Propylene Glycol Butyl Ether | 5131-66-8 | ≤ 5%
Tetrapotassium Pyrophosphate | 7320-34-5 | ≤ 1%
Potassium Silicate | 1312-76-1 | ≤ 1%
Colorant | Proprietary | ≤ 1%

## Slide 6: Results
Summary of Testing
Break in and initial diagnostics normal
Baseline normal
Diagnostics after baseline normal
Steady rapid decay during contamination ~22 mV/hr
Diagnostics after contamination abnormal
Limited recovery ~119 mV, asymptote at ~500 mV
Diagnostics after clean up show limited improvement

## Slide 7: Results (cont)
Test Results:
Figure 1 shows the performance history.
Figure 2 shows no change in IR until attempting clean up.
Figure 3A (anode) and Figure 3C (cathode) show no decay due to crossover.
Figure 4A (anode) and Figure 4C (cathode) show no catalyst issues
However, the Electrochemical impedance spectroscopy (EIS) shown in Figure 5 is very interesting

## Slide 8: Results (cont)
Figure 1 – Performance History
Rapid decay starts upon exposure.
Linear decrease during exposure.
Partial clean up on DI water until asymptotes

## Slide 9: Results (cont)
Figure 2 – IR History
Initial step change due to intentional ‘flooding’.
Linear increase during exposure.
Partial clean up on DI water until asymptotes

## Slide 10: Results (cont)
Figure 3 – X/O History
Beginning of Test and End of Test data basically the same.

## Slide 11: Results (cont)
Figure 4 – Cyclic Voltammetry History
Beginning of Test and End of Test data basically the same.

## Slide 12: Results (cont)
Figure 5 – Electrochemical impedance spectroscopy (EIS)

## Slide 13: Results (cont)
Test Results (cont):
The difference between the measurements at the beginning of the test and beginning of contamination are slight and may be due to saturation of the cathode GDL.
The difference between the measurements at the beginning of contamination and end of contamination are notable.
Frequency magnitude from right to left.
  Right is 0.1 Hz and represents issues in mass transport issues
  Left is 10 kHz and represents ionic and ohmic resistance
Looks to be mass transport issues.
The difference between the measurements at the end of contamination and end of test are also notable. They mirror the recovery.

## Slide 14: What does this mean?
Assumptions:
  Ingest 14 cc’s of 100% cleanser during a 7 kg fill
  Operate at ~1/4 power (1000 mA/cm2) for 14 hrs (est. range on 7 kg)
Results:
  Operating at extreme conditions
  Assumptions may be too conservative
  Decay is 0.2 mV/hr @1000 mA/cm2 prior to contamination
  Decay is ~22 mV/hr @1000 mA/cm2 duringto contamination
  Clean up consisted of injecting DI water. There was a partial recovery.
  The EIS also improved. This may indicates mass transport issues.